Supplementary information

TITLE:

Production of stable monodisperse phospholipid-coated microbubbles at room temperature using a microfluidic flow-focusing device

AUTHORS AND AFFILIATIONS:

Yuchen Wang1, Benjamin R. G. Johnson2, Klazina Kooiman1

1Biomedical Engineering, Department of Cardiology, Cardiovascular Institute, Erasmus MC, Rotterdam, NL

2Molecular and Nanoscale Physics Group, School of Physics and Astronomy, University of Leeds, Leeds, UK

Fabrication of master mold
Device masters were fabricated using 3-inch silicon wafers and the negative photoresist SU-8 2025 (Microchem, Warwickshire, UK). Before use, wafers were rinsed with isopropanol (IPA) and dried using a nitrogen gun before being placed in an oven at 180 ⁰C for ~ 20 mins, to remove excess moisture. Room temperature wafers were placed on a spin coater (EMS 6000, Electronic Micro Systems, UK) and coated with SU-8, and then the acceleration, speed and spin times were set to achieve the desired photoresist thickness. To achieve a desired thickness of ~ 25 μm and ensure an even coating of SU-8, the following spin profile was used.

| Step | Speed (RPM) | Acceleration (RPM/s) | Time (s) |
| --- | --- | --- | --- |
| 1 | 200 | 100 | 5 |
| 2 | 400 | 100 | 5 |
| 3 | 600 | 100 | 5 |
| 4 | 2250 | 100 | 30 |
| End | 0 | 100 | - |

A soft bake step was used to solidify the SU-8 layer by evaporating the solvent in the SU-8. Wafers were placed on a room temperature hot plate (EMS 1000-1, Salisbury, UK) which was then set to 55 ⁰C (it took ~5 min for the hot plate to heat to 55 ⁰C). Wafers were left at 55 ⁰C for 30 mins before turning the hot plate off and waiting for them to cool to room temperature. Direct-write laser lithography was used to etch the microfluidic design into the SU-8 using a 375 nm wavelength laser with a 2 μm resolution, and a laser dose of 250 mJ/cm2 (MicroWriter ML, Durham Magneto Optics, UK). A post-exposure bake completed the polymerisation of the SU-8, following the same parameters as the soft bake. Wafers were developed in ethyl lactate solvent (EC solvent) for ~ 2 mins to remove the un-crosslinked SU-8, then washed in (IPA) for ~ 1 min. If the IPA wash resulted in a cloudy solution, the wafer was developed for a further 30 s in EC solvent, before washing in IPA. This step was repeated until the IPA wash was completely clear, signifying complete development of any un-crosslinked SU-8. The height of the SU-8 channels was confirmed using a Stylus Profiler (Dektak, Bruker, USA).

Schematic of the chip design

Figure S1. Schematic of the chip design with the main chip dimensions summarized in the table. This image has been reproduced with permission from Abou-Saleh et al. 20211.

Reference:

1	Abou-Saleh, R. H. et al. Horizon: Microfluidic platform for the production of therapeutic microbubbles and nanobubbles. Rev Sci Instrum. 92 (7), dae (2021).